# SECTION 03 35 33 – STAMPED CONCRETE FINISHING

# Concrete Sealers

SPECIFIER NOTE: THESE SPECIFICATIONS WERE CURRENT AT THE TIME OF PUBLICATION BUT ARE SUBJECT TO CHANGE AT ANY TIME WITHOUT NOTICE.  PLEASE CONFIRM THE ACCURACY OF THESE SPECIFICATIONS WITH THE MANUFACTURER AND/OR DISTRIBUTOR PRIOR TO CONSTRUCTION OR INSTALLATION.

GUIDE SPECIFICATIONS:

THIS GUIDE SPECIFICATION IS WRITTEN ACCORDING TO THE CONSTRUCTION SPECIFICATIONS INSTITUTE (CSI) FORMATS, INCLUDING MASTERFORMAT®, SECTIONFORMAT™, AND PAGEFORMAT™.

CAREFULLY REVIEW AND EDIT THIS SECTION TO MEET THE REQUIREMENTS OF THE PROJECT, LOCAL BUILDING CODE AND AUTHORITIES HAVING JURISDICTION. COORDINATE THIS SECTION WITH OTHER SPECIFICATION SECTIONS AND DRAWINGS.

DELETE ALL "SPECIFIER NOTES" WHEN EDITING THIS SECTION.

# GENERAL

## CONDITIONS AND REQUIREMENTS

### The General Conditions, Supplementary Conditions, and Division 01 – General Requirements apply.

## SECTION INCLUDES

## Section 03 35 33 – Stamped Concrete Finishing products of the following types:

*********************************************************************************************************************************************
SPECIFIER NOTES: RETAIN ONLY THOSE ITEMS BELOW THAT REMAIN AFTER EDITING TEXT OF SECTION.

*********************************************************************************************************************************************

### TS200 Acrylic Topical Sealer SB-25 with High Gloss Sealer.

### TS201 Acrylic Topical Sealer SB-25 with High Gloss Sealer.

### TS202 Acrylic Topical Sealer WB-25 with Low Gloss Sealer.

## RELATED SECTIONS

### Section 03 01 00 – Maintenance of Concrete.

### Section 03 30 00 – Cast-in-Place Concrete.

### Section 03 35 00 – Concrete Finishing.

### Section 03 35 13 – High-Tolerance Concrete Floor Finishing.

### Section 03 35 16 – Heavy-Duty Concrete Floor Finishing.

### Section 03 35 43 – Polished Concrete Finishing.

### Section 07 19 00 – Water Repellents.

### Section 09 60 00 – Flooring.

### Section 09 96 00 – High-Performance Coatings.

### Section 09 96 35 – Chemical Resistant Coatings.

### Section 09 97 00 – Special Coatings.

### Section 09 97 23 – Concrete and Masonry Coatings.

### Section 32 13 13 – Concrete Paving.

### Section 32 13 16 – Decorative Concrete Paving.

### Section 32 13 16.13 – Patterned Concrete Paving.

### Section 32 13 16.19 – Imprinted Concrete Paving.

### Section 32 13 16.23 – Stamped Concrete Paving.

## REFERENCES

****************************************************************************************************************************************
SPECIFIER NOTES: REFERECE STANDARDS APPLIED SHALL REFLECT THE DATE OF THE STANDARD THAT IS IN EFFECT AS OF THE DATE OF RECEIPT OF BIDS FOR THE PROJECT.  RETAIN ONLY THOSE REFERENCES THAT ARE REQUIRED AFTER THE SECTION IS EDITED

****************************************************************************************************************************************

### Abbreviations and Acronyms EPA:

### U.S. Environmental Protection Agency.

### FDA: U.S. Food and Drug Administration.

### OSHA: Occupational Safety and Health Administration.

### VOC: Volatile Organic Compound.

### Reference Standards

### AASHTO (The American Association of State Highway and Transportation Officials):

### AASHTO M148: Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete

### ASTM International (ASTM):

#### ASTM C156: Standard Test Method for Water Loss [from a Mortar Specimen] Through Liquid Membrane-Forming Curing Compounds for Concrete.

#### ASTM C309: Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete.

#### ASTM C1315: Standard Specification for Liquid Membrane-Forming Compounds Having Special Properties for Curing and Sealing Concrete.

#### ASTM D1653: Standard Test Methods for Water Vapor Transmission of Organic Coating Films.

## SUBMITTALS

### Product Data:

#### Submit manufacturer's printed product literature, specifications, technical data sheet and safety data sheet for all products used.

#### Submit manufacturer’s application and repair instructions.

#### Submit manufacturer’s storage and handling recommendations.

*********************************************************************************************************************************************

SPECIFIER NOTES: DELETE IF NOT APPLICABLE TO PROJECT.

*********************************************************************************************************************************************

### Shop Drawings: Include details of materials, construction, and finish.

## QUALITY ASSURANCE

### Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum of ten years documented experience.

### Installer Qualifications: Company specializing in performing Work of similar scope with minimum two years documented experience.

### Source Limitations: Provide each type of product from a single manufacturing source.

*********************************************************************************************************************************************

SPECIFIER NOTES: MOCK-UPS AND PRE-APPLICATION CONFERENCES SHOULD BE INCLUDED IF THE PROJECT SIZE WARRANTS THE EXPENSE. DELETE IF NOT APPLICABLE TO PROJECT.

*********************************************************************************************************************************************

### Mock-Ups: Construct mock-up of actual materials for review and approval by Architect.  Provide mock-ups in sufficient time so as not to delay construction progress.  If the mock-up is not deemed acceptable by the Architect, rebuild the mock-up until it is deemed acceptable by the architect.

### Pre-Application Conference: Convene a conference including the Architect and Contractor at least 14 days prior to starting application. Review the schedule, responsibilities, critical items, and approvals.

## DELIVERY, STORAGE AND HANDLING

### Store and handle in accordance with the manufacturer’s recommendations.

### Protect sealer containers from damage due to weather, excessive temperature, and construction operations.

## FIELD [OR] SITE CONDITIONS

## Do not install products under environmental conditions outside of the manufacturer’s recommended limits.

## WARRANTY

### Manufacturer’s Warranty: Provide manufacturer’s standard limited warranty in effect at the date of purchase.

# PRODUCTS

## MANUFACTURERS

### Specified Manufacturer: Concrete Sealers USA, PO Box 5464, De Pere, WA. 885-583-2991. Email: info@concretesealerusa.com; Web: www.concretesealersusa.com.

*********************************************************************************************************************************************

SPECIFIER NOTES: DELETE ONE OF THE FOLLOWING TWO PARAGRAPHS.

*********************************************************************************************************************************************

### Substitutions: Not Permitted.

### Requests for approved substitutions will be considered in accordance with provisions specified in Section 01 62 00 – Product Options.

*********************************************************************************************************************************************

SPECIFIER NOTES: MATERIALS AND PRODUCTS ARE INDICATED IN THE FOLLOWING PARAGRAPHS. OPTIONS WITHIN ARE INDICATED BY SQUARE BRACKETS. DELETE PARAGRAPHS AND OPTIONS NOT REQUIRED FOR THIS PROJECT.

*********************************************************************************************************************************************

## MATERIALS: STAMPED CONCRETE FINISHING

### Stamped Concrete Finishing Products: Topical sealers designed for finishing newly placed and existing stamped concrete surfaces.

### Product Basis of Design: TS200 Acrylic Topical Sealer SB-25 with High Gloss Sealer manufactured by Concrete Sealers USA.

#### Product Description: TS200 is a high VOC, solvent based curing agent and sealer for decorative concrete, pavers, and exposed concrete. TS200 is a 25 percent solids high performance proprietary formulation of pure acrylic polymer resin in a less than 700 gram per liter VOC solvent base.  TS200 is designed to provide color enhancement, a high gloss finish, protection from freeze and thaw cycles, is UV resistant, non-yellowing, restrict water, reduce dirt build up, stains, reduce mold and mildew, blocks efflorescence, reduce scaling and spalling and increase surface durability.

#### Performance Characteristics:

#### Complies with AASHTO M148 Curing Concrete: Type 1, Class A and B.

#### Complies with ASTM C156 Moisture Retention: 0.035 grams per cubed centimeter.

#### Complies with ASTM C309 Curing Concrete: Type 1, Class A and B.

#### Complies with ASTM C1315 Curing and Sealing Concrete: Type 1, Class A.

#### Usage: Sealing stamped concrete.

#### Environmental and Regulatory:

#### OSHA Hazard Communication Standard: Hazardous under 29CFR 1910.1200.

#### VOC Content: 700 gram per liter VOC.

#### Composition: Pure Acrylic Resin Suspended in Solvent.

#### Solids: 25 percent.

#### Carrier Type: Solvent based.

#### Specific Gravity (H2O = 1): 0.92.

#### Percent Volatile by Volume: Less than 700 grams per liter.

#### Flashpoint: 105 degrees Fahrenheit (40.6 degrees Celsius).

#### Flammable Limits:

#### Lower Limit: 0.9 percent.

#### Upper Limit: 6.2 percent.

#### Finish: High gloss.

#### Color: [Clear] or [Color tints are available from the manufacturer].

#### Odor: Solvent odor.

#### Approximate Coverage Rates:

#### Initial Coat Cure and Seal: 200 to 300 square feet per gallon.

#### Additional Coats Cure and Seal: 300 to 400 square feet per gallon.

#### Initial Coat Existing Substrates: 300 to 400 square feet per gallon.

#### Additional Coats Existing Substrates: 300 to 400 square feet per gallon.

#### Approximate Drying Time:

#### To Touch: 1 to 2 hours.

#### Traffic: 4 to 6 hours.

#### Wheel Traffic: 24 to 48 hours.

#### Re-Coat Time: 4 to 6 hours.

#### Blush Resistance: Good.

#### Solvent Resistance: Minimal.

#### Concrete Adhesion: Excellent.

#### Shelf Life: 3 years unopened in protected storage.

### Product Basis of Design: TS201 Acrylic Topical Sealer SB-25 with High Gloss Sealer manufactured by Concrete Sealers USA.

#### Product Description: TS201 is a low VOC, solvent based curing agent and sealer for decorative concrete, pavers, and exposed aggregate. TS201 is a 25 percent solids high performance proprietary formulation of pure acrylic polymer resin in a less than 350 gram per liter VOC solvent base.  TS201 is designed to provide color enhancement, a high gloss finish, protection from freeze and thaw cycles, is UV resistant, non-yellowing, restrict water, reduce dirt build up, stains, reduce mold and mildew, blocks efflorescence, reduce scaling and spalling and increase surface durability.

#### Performance Characteristics:

#### Complies with AASHTO M148 Curing Concrete: Type 1 and 1D, Class A and B.

#### Complies with ASTM C156 Moisture Retention: 0.035 grams per cubed centimeter.

#### Complies with ASTM C309 Curing Concrete: Type 1, Class A and B.

#### Complies with ASTM C1315 Curing and Sealing Concrete: Type 1 and 2, Class A.

#### Usage: Sealing stamped concrete.

#### Environmental and Regulatory:

#### OSHA Hazard Communication Standard: Hazardous under 29CFR 1910.1200.

#### VOC Content: Less than 350 gram per liter VOC.

#### Composition: Pure Acrylic Resin Suspended in Solvent.

#### Solids: 25 percent.

#### Carrier Type: Solvent based.

#### Specific Gravity (H2O = 1): 1.0.

#### Percent Volatile by Volume: Less than 350 grams per liter.

#### Boiling Point: 194 degrees Fahrenheit (90 degrees Celsius)

#### Flashpoint: 68 degrees Fahrenheit (20 degrees Celsius).

#### Flammable Limits:

#### Lower Limit: 1.0 percent.

#### Upper Limit: 7.0 percent.

#### Finish: High gloss.

#### Color: [Clear] or [Color tints are available from the manufacturer].

#### Odor: Solvent odor.

#### Approximate Coverage Rates:

#### Initial Coat Cure and Seal: 250 to 350 square feet per gallon.

#### Additional Coats Cure and Seal: 300 to 400 square feet per gallon.

#### Initial Coat Existing Substrates: 300 to 400 square feet per gallon.

#### Additional Coats Existing Substrates: 300 to 400 square feet per gallon.

#### Approximate Drying Time:

#### To Touch: 1 to 2 hours.

#### Traffic: 4 to 6 hours.

#### Wheel Traffic: 24 to 48 hours.

#### Re-Coat Time: 4 to 6 hours.

#### Blush Resistance: Good.

#### Solvent Resistance: Minimal.

#### Concrete Adhesion: Excellent.

#### Shelf Life: 2 years unopened in protected storage.

### Product Basis of Design: TS202 Acrylic Topical Sealer WB-25 with Low Gloss Sealer manufactured by Concrete Sealers USA.

#### Product Description: TS202 is a low VOC, water based curing agent and sealer for decorative concrete, pavers, and exposed aggregate. TS202 is a 25 percent solids high performance proprietary formulation of pure acrylic polymer resin in a less than 100 gram per liter VOC water base.  TS202 is designed to provide color enhancement, a low gloss satin finish, protection from freeze and thaw cycles, is UV resistant, non-yellowing, restrict water, reduce dirt build up, stains, reduce mold and mildew, blocks efflorescence, reduce scaling and spalling and increase surface durability.  As a joint sand stabilizer, TS202 keeps pavers in place, prevents joint sand erosion, and reduces the growth of weed.  TS202 has a milky white appearance. The substrate will have a low gloss finish when dry.

#### Performance Characteristics:

#### Complies with AASHTO M148 Curing Concrete: Type 1 and 1D, Class A and B.

#### Complies with ASTM C156 Moisture Retention: 0.042 grams per cubed centimeter.

#### Complies with ASTM C309 Curing Concrete: Type 1 and 1D, Class A and B.

#### Complies with ASTM C1315 Curing and Sealing Concrete: Type 1 and 2, Class A.

#### Complies with ASTM D1653 Moisture Vapor Transmission: Less than 0.5 milligrams per cubed centimeter in 24 hours.

#### Complies with CRD5250 Abrasion Test: 21.77 grams weight loss.

#### Usage: Sealing stamped concrete.

#### Environmental and Regulatory:

#### OSHA Hazard Communication Standard: Non-hazardous under 29CFR 1910.1200.

#### VOC Content: Less than 100 gram per liter VOC.

#### Composition: Pure Acrylic Resin Suspended in Water.

#### Solids: 25 percent.

#### Carrier Type: Water based.

#### Specific Gravity (H2O = 1): 1.03.

#### Percent Volatile by Volume: Less than 100 grams per liter.

#### Boiling Point: 212 degrees Fahrenheit (100 degrees Celsius).

#### Flashpoint: 212 degrees Fahrenheit (100 degrees Celsius).

#### Finish: Low gloss.

#### Color: Clear to milky white.

#### Odor: Mild.

#### Approximate Coverage Rates:

#### Initial Coat Cure and Seal: 250 to 350 square feet per gallon.

#### Additional Coats Cure and Seal: 300 to 400 square feet per gallon.

#### Initial Coat Existing Substrates: 300 to 400 square feet per gallon.

#### Additional Coats Existing Substrates: 300 to 400 square feet per gallon.

#### Approximate Drying Time:

#### To Touch: 1 to 2 hours.

#### Traffic: 4 to 6 hours.

#### Wheel Traffic: 24 to 48 hours.

#### Re-Coat Time: 4 to 6 hours.

#### Blush Resistance: Good.

#### Solvent Resistance: Superior.

#### Concrete Adhesion: Excellent.

#### Shelf Life: 2 years unopened in protected storage.

# EXECUTION

## EXAMINATION

### Examine Project conditions and completed Work and verify that substrates have been properly prepared.

### If another installer is responsible for preparing the substrate, notify the Architect in writing of unsatisfactory substrate.

### Immediately correct all deficiencies and conditions which would cause improper execution of Work specified in this Section and subsequent Work.

### Proceeding with Work specified in this Section shall be interpreted to mean that all conditions were determined to be acceptable prior to start of Work.

## PREPARATION

### Protection: All surfaces must be clear of dirt and debris.

### Surface Preparation: Refer to the manufacturer’s recommendations for appropriate substrate method preparation under the project conditions.

### Sealer Storage: Sealers shall be kept in tightly closed containers in a dry, cool, and well ventilated location. Adhere to the manufacturer’s recommendations for storage and handling.

## APPLICATION

### Apply Concrete Sealers USA’s sealer in accordance with manufacturer instructions and recommendations and the authorities having jurisdiction.

### Use in accordance with approved submittals and in proper relationship with adjacent construction.

## FIELD QUALITY CONTROL

### Field Testing and Inspection: Field inspection will be performed as specified in Section 01 45 00 – Quality Control.

### Corrective Actions: Replace or repair Work to eliminate defects, deficiencies, and irregularities.

### Manufacturer’s Field Services: Provide field [instruction] [inspection] services by manufacturer or authorized agent of the manufacturer in accordance with general requirements specified in Section 01 60 00 – Product Requirements.

## ADJUSTMENT AND CLEANING

### Clean products in accordance with manufacturer’s recommendations.

### Repair, touch-up, or replace damaged products prior to Substantial Completion.

# END OF SECTION