Teak Shield
Use to shield teak from stains and markings
1. Before using the Teak Shield, eye protection and rubber gloved should be worn. Cover the ground under your work area before starting.
2. New Teak: First clean without Teak Cleaner to remove some of the natural teak oils (or weather for 2 weeks outside before treatment).
3. Before using the Teak Shield on dark gray teak, clean the wood with Teak Cleaner. If cleaned wood feels rough, sand lightly before treating with Teak Shield.
4. Make sure the teak is 100% dry and free of dust.
5. Shake for at least one minute before use. Apply a thin layer of Teak Shield with a soft cloth.
6. Allow to dry for 4 hours and then apply a second thin coat of Teak Shield. Let the teak dry for 48 hours before exposure to moisture.
7. It is recommended that you treat your teak furniture with Teak Shield once a year. Tabletops should be treated more often.


